## Slide 1
lightform.org.uk
Adam Plowman, João Quinta da Fonseca, Pratheek Shanthraj
TiFUN Progress Meeting, 07/12/2021
Developing a modelling pipeline for hot-rolling of dual-phase titanium

## Slide 2
Aims
Develop modelling tools for investigating hot-deformation of dual-phase Ti alloys
Help us to understand:
  co-deformation of two phases
  texture and microstructural evolution
  dynamic transformation: globularisation and grooving
Integration with experimental data

## Slide 3
Strategy
Deformation
Recovery
RX
Part 1: static modelling
(evolution after deformation)
deform with crystal plasticity (DAMASK)
cluster orientations to identify grains
evolve microstructure with phase field (CIPHER)
time
Notes: With static, we impose a recovery structure using reasonable empirical relations (from orientation clustering)

## Slide 4
Strategy
Deformation
Recovery
RX
Part 1: static modelling
(evolution after deformation)
deform with crystal plasticity (DAMASK)
cluster orientations to identify grains
evolve microstructure with phase field (CIPHER)
time
Part 2: dynamic modelling
(evolution during deformation)
coupled crystal-plasticity/phase-field model (DAMASK)
time

## Slide 5
Methods: crystal plasticity (CP)
Simple phenomenological power law
Slip rate on slip system :
Reference slip rate
Resolved shear stress
Resistance to slip (CRSS)
Stress exponent
In general, evolves from to
https://damask.mpie.de/
Finite-strain CP
Generalised material-point continuum model
IN: deformation gradient,
OUT: 1st Piola-Kirchoff stress,
via constitutive law, such as…
Notes: Can change to different laws
Since generalised, we can add in support for phase-field evolution

## Slide 6
Methods: phase field (PF)
Microstructure evolution:
Solute diffusion:
Thermal conduction:
Gibbs energy  CALPHAD databases
Interface mobility  needs to be calibrated
Solute mobility  Diffusion databases/needs calibration
Thermal properties  needs calibration
Multi-phase field theory
Notes: interface mobilities: from diffusion-controlled assumption for growth
solute mobilities/driving forces: from CALPHAD databases
interface energies: probably not so important; transformation driven by stored energy more than capillary effects

## Slide 7
Methods: PF with CIPHER
Efficient grand-canonical-based phase-field implementation, using:
Compound Energy Formalism
Other CALPHAD thermodynamic models for multi-component system
CIPHER: Phase-field simulation code for microstructure evolution in multi-component alloy systems
✔ Automatic parallel adaptive mesh refinement
✔ MPI parallelization and scalability
✔ Large number of phases (10-10,000); constant computational complexity
✔ Local truccation error estimates and adaptive time stepping
✔ Open-source: https://github.com/micmog/CIPHER

## Slide 8
load to 40%
-soft direction
Results: phase-field pre-processing
Orientation clustering
-hard direction
plane
Fast multi-scale clustering
arbitrary colouring
Notes: Loading direction is one “variable”: lots of others to look at later (e.g. surface roughness, volume fraction, real vs synthetic microstructures)
𝜌 perhaps inaccurate due to room temperature single crystal parameters?

## Slide 9
-soft direction
Results: phase-field pre-processing
Dislocation density
-hard direction
plane
estimate [1] dislocation density, :
: constant
: shear modulus
: Burgers vector
Dislocation density,
3e16
8e16
3e16
11e16
[1] Empirical equation. See: Humphreys, F. J., and M. Hatherly. ‘Chapter 2 - The Deformed State’. https://doi.org/10.1016/B978-008044164-1/50006-2.
load to 40%
Notes: perhaps inaccurate due to room temperature single crystal parameters?
𝜌 perhaps inaccurate due to room temperature single crystal parameters?

## Slide 10
Results: phase-field pre-processing
Tessellation of sub-grains
-hard direction
Dislocation density,
3e16
8e16
3e16
11e16
Clustered grains
Estimate [1] cell diameter:
: cell diameter
: dislocation density
: constant ~1000
Choose a pixel length: μm
Calculate cell density (number per area), :
Cell density, , is then a probability field from which we sample seed points
[1] Humphreys, F. J., and M. Hatherly. Chapter 13 – ‘Hot Deformation and Dynamic Restoration’ https://doi.org/10.1016/B978-008044164-1/50017-7
plane
-soft direction
Notes: Now want to distribute seed points within each grain, representing the seeds of dislocation cells/sub-grains

## Slide 11
Results: phase-field pre-processing
Tessellation of sub-grains
plane
-soft direction
-hard direction
arbitrary colouring
LAGB
HAGB
LAGB
interface colouring
 | GB energy / J m-2 | GB mobility / m3 J-1 s-1
HAGB | 0.5 | 1e-11
LAGB | 0.2 | 5e-11

## Slide 12
Results: PF grain-growth
Tessellation of sub-grains
-soft direction
-hard direction
LAGB
HAGB
LAGB
interface colouring

## Slide 13
2022 plan
Synthetic microstructures
Real microstructures
Variables:
Loading directions
Synthetic vs. real microstructures
Surface roughness
Particle volume fraction
Full MatFlow integration for future-proofing
Part 2: dynamic modelling
Extend DAMASK to provide CP/PF coupling
Re-examine investigates from Part 1
Output: paper demonstrating coupled modelling to explain experimental observations (e.g. grooving)
Part 1: static modelling
Include effect of chemistry (currently just microstructure evolving)
For two phases: growth depends on how fast Al, V are diffusing
Interface mobilities from diffusion-controlled assumption for growth
CIPHER

## Slide 14
-hard direction
plane
-soft direction
Clustered misorientation distributions